| General-purpose Resistors/Carbon Film Resistors |  |
| --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. General purpose; CF; Carbon film; 0.25, 0.5; 2.2 5.1M; 2, 5. CFP; Carbon film (Flame retardant); 0.25, 0.5; 2.2 1M; 2, 5.

|  | Precision Resistors/Metal Film Resistors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Precision; MF; Metal film (Precision, Low T.C.R.); 0.25, 0.5; 0.51 5.11M; 0.5, 1, 2. SN; Metal film (Precision, Low T.C.R.); 1, 2; 4.99 1.5M; 0.5, 1, 2. MFP; Metal film (Flame retardant); 0.25, 0.5; 10 100k; 1. SNF; Metal film (Flame retardant); 0.25, 0.5; 0.47 100; 5. MRS; Metal film (Radial); 0.125 0.3; 10 - 1M; 0.01, 0.02, 0.05, 0.1, 0.25, 0.5. LF; Metal film (L-shape lead); 0.125 0.5; 1 1M; 0.5, 1, 2,5. LFF; Metal film (Flame retardant, L-shape lead); 0.25; 1 100k; 1, 2. RNS; Metal film (Precision, Low T.C.R.); 0.125 1; 0.2 6.8M; 0.1,0.25,0.5,1. SF; Metal film (Molded, High precision); 0.125 0.5; 100 5.11M; 0.01, 0.02, 0.05, 0.1, 0.25, 0.5.

|  | Resistors for High Voltage Circuit |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. High voltage; RK; Metal glaze film; 0.25 1; 100k 100M; 1, 2, 5. RK1/2G; Discharge path resistor (UL1676); 0.5; 1M 12M; 5. RK26; Metal glaze film (L - shape lead); 0.25; 100k 33M; 1, 2, 5. RCR; Anti surge resistors (UL1676)/(EN60065); 0.25 3; 3.3 100M; 1, 5. GS; High voltage, High power; 0.25 12; 500k 10G; 0.5, 1, 2, 5, 10. RK92; High voltage (Metal glaze film); 0.5 1.1; 1M 1G; 1, 2, 5, 10, 20. PCF; Anti surge・pulse ceramic resistor; 0.5 2; 3.3 390k; 10, 20. HPC; Anti surge・pulse ceramic resistor; 0.5 5; 3.3 390k; 10, 20. CPCN; Ceramic resistor; 0.5 2; 1k 15k; 20. P; High voltage; 1.5 250; 10 6G; 5, 10, 20.

|  | Power Type Resistors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Power; MOS; Metal oxide film (Small size); 0.5 5; 10 100k; 1, 2, 5. MOSX; Metal film (Small size); 0.5 5; 0.1 9.1; 1, 2, 5. MO; Metal oxide film; 0.5 3; 10 150k; 2, 5. MOX; Metal film; 0.5 3; 0.2 9.1; 2, 5. SPR; Special power resistor; 0.25 5; 2.2 1M; 1, 2, 5. SPRX; Metal film (Small size); 0.25 5; 0.1 2; 5. BGR; Cement case (Wire wound, Glass core); 5 40; 0.39 390; 5, 10. BWR; Cement case (Wire wound, Ceramic core); 1 20; 0.1 390; 1, 2, 5. BSR; Cement case (Metal oxide film); 2 20; 430 75k; 5.

|  | Wirewound Resistors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Wire wound; CW; Wire wound; 0.25 5; 0.01 390; 0.25, 0.5, 1, 2, 5, 10. CW-H; Wire wound; 1 3; 0.1 3k; 0.5, 1. RW; Wire wound (Precision, Low T.C.R.); 0.5 10; 0.1 62k; 0.5, 1, 3, 5.

|  | Current Sense Resistors/Low Resistance Resistors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Low resistance; BPR; Cement case (Metal plate); 2 10, 5+5, 7+7; 0.01 1; 5, 10. LR; Metal wire; —; 3m 100m; 3, 5.

|  | Resistor Networks/Resistor Array |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Network; MRP; Thin film R network (Balance resistors); 100m; 50 100k; 0.1, 0.25, 0.5, 1. RKL; Thick film R network (Low profile); 125m, 200m; 22 1M; 1, 2, 5. RKC; Thick film R network (Standard); 20m 250m; 22 2.2M; 1, 2, 5. RKH; Thick film R network (Power type); 250m, 500m; 56 2.2M; 1, 2, 5.

|  | Linear P.T.C. Resistors/Thermal sensers |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Linear; LT; Linear PTC; 0.16, 0.25; 10 51k; 2, 5. LP; Linear PTC (Precision); 0.063, 0.125; 1 100k; 1, 2, 5.

|  | Platinum Thin Film Thermal Sensors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Platinum thin film thermal sensors; SDT101; Platinum thin film ,thermal sensors; 0.125; 10, 100, 500; 0.5, 1. SDT310; Platinum thin film ,thermal sensors (L-shape lead); —; 10,100, 500, 1k; 0.059, 0.12, 0.39,10.

|  | Fusing Resistors |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Fusible; RF; Fusing resistor; 0.17 2; 0.1 15k; 5. RF26; Fusing resistor (L-shaped lead); 0.25; 0.1 1k; 5. RF25CC; Fusing resistor (Constant current fusing type); 0.25; 0.1 0.91; 10. WF; Thermal fuse built-in resistor; 1.2 3.5; 1 10k; 5, 10.

|  | Jumper Wires |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. Jumper; Z; Jumper (Coating type); —; 20m max.; —. J-Z; Jumper (Molded); —; 10m max.; —. JL; Jumper wire (Taping); —; —; —.

|  | CR Networks |  |
| --- | --- | --- |

Category; Type; Features; Power Rating (W); Resistance Range(Ohm); Tolerance (%); PDF. CR; CR; Thick film C/R network (Customorders); —; 10 1M; 5.

Common Specification. Items; PDF. Minimum Ordered Quantity. Recommended Pad Dimensions. Packagings For Chip Components. Axial Tapings. Radial Taping. Forming. Color code•Resistance marking•E series numbers..