ALUMINUM  ELECTROLYTIC  CAPACITORS                                                      M.D.L.

TE  Series

AXIAL  Type  85℃

█  FEATURES

.85℃,2,000 hours assured

. Voltage range of 6.3 ~ 450V

.Wide operating temperature range,from -40℃~ +85℃

█  SPECIFICATION

| Item | Characteristic |  |
| --- | --- | --- |
| Operation Temp 使用溫度範圍 | -40℃ ~ +85℃ |  |
| Capacitance Tolerance 容量範圍 | ±10%(K), ±20%(M) (at 20℃,120Hz) |  |
| Rated Voltage 額定電壓 | 6.3 ~ 100VDC | 160 ~ 450VDC |
| (20℃) Leakage Current 洩漏電流 | I≦0.02CV or 3 (u A)Whichever is greater 選其最大值 (after 2 minutes applying the rated DC working Voltage at 20 ℃)(在20℃施加直流額定電壓2分鐘以後) | I≦0.03CV+15 (u A) for CV≦1000, I≦0.02CV+25 (u A) for CV>1000 (after 5 minutes applying the rated DC working Voltage at 20 ℃)(在20℃施加直流額定電壓5分鐘以後) |
|  | Where: I=Leakage Current (u A) , C=rated Capacitance (μ F) , V= working Voltage (V) |  |
| (at 20℃,120Hz) Dissipation Factor (tan δ) 損失角 | W.V; 6.3; 10; 16; 25; 35; 50; 63; 100; 160; 200; 250; 350; 400; 450. tan δ; 23; 20; 0.17; 0.15; 0.12; 0.10; 0.09; 0.08; 0.15; 0.15; 0.20; 0.20; 0.24; 0.24. Add 0.02 per 1000μ F for more than 1000μ F (當靜電容量超過1000μ F時，容量每增加1000μ F，損失角正切值就增加0.02) |
| (20℃) Surge Voltage 突破電壓 | W.V; 6.3; 10; 16; 25; 35; 50; 63; 100; 160; 200; 250; 350; 400; 450. S.V; 8; 13; 20; 32; 44; 63; 79; 125; 200; 250; 300; 400; 450; 500. |
| Low Temperature Stability 低溫溫度特性 | Impedance ratio at 120 HZ 阻抗測試頻率為120Hz Rated Voltage (V); 6.3; 10; 16; 25; 35; 50; 63; 100; 160; 200; 250; 350; 400; 450. Z(-25℃) /+20℃; ∮D<16; 6; 4; 3; 3; 2; 2; 2; 2; 3; 6; 8; 12; 14; 16. ∮D≥16; 8; 6; 4; 4; 3; 3; 3; 3. Z(-40℃) /+20℃; ∮D<16; 10; 8; 6; 6; 4; 3; 3; 3; 4; 8; 10; -; -; -. ∮D≥16; 18; 16; 12; 10; 8; 8; 6; 6. |
| Load Life Test 高溫負荷壽命 | After 2,000 hours application of rated voltage at 85℃,capacitors meet the characteristics requirements listed as below .在額定電壓85℃條件下，經過2,000小時後，電容特性要求如下表： Capacitance Change; Within ±20% of initial value. Dissipation Factor; Less than200% of specified value. Leakage Current; Within specified value. |
| Shelf Life Test 無負荷壽命 | After leaving capacitors under no load at 85℃ for 1,000 hours and applying Voltage they meet the specified value for load life characteristics listed above .將電容器置於溫度為85℃、無電壓負荷狀況下，經過1,000小時後，再加電壓於電容器，其所測值標準應與有負荷時測試值相同。 |  |
| Frequency Coefficient of Allowable Ripple Current 允許紋波電流的頻率係數 | Freq.(Hz) Cap.( μ F); 60; 120; 500; 1K; 10K up. Under 100; 0.70; 1.00; 1.30; 1.40; 1.50. 100 to 1000; 0.75; 1.00; 1.20; 1.30; 1.35. 1000 up above; 0.80; 1.00; 1.10; 1.12; 1.15. |
| Allowable Ripple Current Vs; Ambient Temperature 環境溫度對比允許紋波電流的比值 | Temperature(℃); Under 50; 70; 85. Multiplier; 1.78; 1.40; 1.00. |

ALUMINUM  ELECTROLYTIC  CAPACITORS                                                      M.D.L.

TE  Series

AXIAL Type  85℃

█ CASE SIZE & Max RIPPLE CURRENT

Dimension Diameter (∮D)×Length(L) mm                                                                        Ripple Current: m A/rms at 85℃,120Hz

尺寸：直徑(∮D) × 長度L (mm)                                                                               紋波電流(m A) : 溫度85℃,測試頻率120Hz

| WV μ F | 6.3V |  | 10V |  | 16V |  | 25V |  | 35V |  | 50V |  | 63V |  | 100V |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C |
| 0.10 |  |  |  |  |  |  |  |  |  |  | 5×12 | 1.5 | 5×12 | 3 | 5×12 | 3 |
| 0.22 |  |  |  |  |  |  |  |  |  |  | 5×12 | 3.5 | 5×12 | 4.5 | 5×12 | 5 |
| 0.33 |  |  |  |  |  |  |  |  |  |  | 5×12 | 5 | 5×12 | 7.5 | 5×12 | 8 |
| 0.47 |  |  |  |  |  |  |  |  |  |  | 5×12 | 6 | 5×12 | 9 | 5×12 | 9 |
| 1.0 |  |  |  |  |  |  |  |  |  |  | 5×12 | 10 | 5×12 | 15 | 5×12 | 15 |
| 2.2 |  |  |  |  |  |  |  |  |  |  | 5×12 | 20 | 5×12 | 30 | 5×12 | 30 |
| 3.3 |  |  |  |  |  |  |  |  |  |  | 5×12 | 30 | 5×12 | 36 | 5×12 | 40 |
| 4.7 |  |  |  |  |  |  |  |  |  |  | 5×12 | 42 | 5×12 | 44 | 6.3×13 | 41 |
| 10 |  |  |  |  |  |  | 5×12 | 40 | 5×12 | 55 | 5×12 | 50 | 6.3×13 | 55 | 6.3×13 | 72 |
| 22 |  |  |  |  | 5×12 | 71 | 5×12 | 76 | 6.3×13 | 70 | 6.3×13 | 85 | 6.3×13 | 109 | 8×16 | 133 |
| 33 |  |  |  |  | 5×12 | 85 | 5×12 | 80 | 6.3×13 | 115 | 6.3×13 | 126 | 8×13 | 154 | 10×17 | 190 |
| 47 | 5×12 | 87 | 5×12 | 94 | 6.3×13 | 88 | 6.3×13 | 100 | 6.3×13 | 138 | 8×13 | 174 | 8×16 | 214 | 10×21 | 237 |
| 100 | 6.3×13 | 121 | 6.3×13 | 145 | 6.3×13 | 160 | 8×13 | 215 | 8×16 | 232 | 10×17 | 296 | 10×17 | 326 | 13×22 | 377 |
| 220 | 6.3×13 | 215 | 8×13 | 231 | 8×13 | 298 | 8×16 | 319 | 10×17 | 401 | 10×21 | 459 | 13×22 | 527 | 16×28 | 625 |
| 330 | 8×16 | 305 | 8×16 | 327 | 8×16 | 365 | 10×17 | 454 | 10×21 | 514 | 13×22 | 613 | 13×22 | 675 | 16×33 | 793 |
| 470 | 8×16 | 364 | 8×16 | 390 | 8×16 | 460 | 10×21 | 524 | 13×22 | 613 | 13×22 | 731 | 13×27 | 780 | 16×36 | 942 |
| 1000 | 10×17 | 662 | 10×17 | 671 | 10×21 | 775 | 13×22 | 873 | 13×27 | 955 | 16×33 | 1111 | 16×36 | 1249 | 22×43 | 1452 |
| 2200 | 13×22 | 929 | 13×22 | 1051 | 13×24 | 1125 | 16×28 | 1344 | 16×33 | 1421 | 18×36 | 1699 | 22×43 | 1744 | 25×52 | 2430 |
| 3300 | 13×27 | 1150 | 13×27 | 1288 | 16×28 | 1454 | 16×33 | 1611 | 18×36 | 1640 | 22×43 | 2027 | 25×52 | 2309 |  |  |
| 4700 | 13×27 | 1354 | 16×28 | 1552 | 16×33 | 1650 | 18×36 | 1881 | 22×43 | 2280 | 25×43 | 2347 | 25×52 | 2710 |  |  |
| 6800 | 16×28 | 1762 | 16×33 | 1930 | 18×36 | 2040 | 18×42 | 2170 | 22×43 | 2470 | 25×52 | 2650 |  |  |  |  |
| 10000 | 16×36 | 2062 | 18×36 | 2122 | 18×42 | 2503 | 22×43 | 2893 | 25×52 | 3180 |  |  |  |  |  |  |

| WV μ F | 160V |  | 200V |  | 250V |  | 350V |  | 400V |  | 450V |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C | SIZE | R.C |
| 1.0 | 6.3×13 | 7 | 6.3×13 | 9 | 6.3×13 | 12 | 8×16 | 13 | 8×16 | 14 | 8×16 | 15 |
| 2.2 | 6.3×13 | 15 | 8×13 | 16 | 8×16 | 17 | 8×21 | 19 | 10×17 | 21 | 10×21 | 23 |
| 3.3 | 8×16 | 21 | 8×16 | 26 | 8×21 | 31 | 8×21 | 33 | 10×17 | 34 | 10×21 | 36 |
| 4.7 | 8×16 | 31 | 10×17 | 33 | 10×17 | 38 | 10×21 | 44 | 10×26 | 45 | 10×26 | 46 |
| 10 | 10×17 | 60 | 10×21 | 66 | 10×21 | 72 | 13×22 | 72 | 13×22 | 80 | 13×27 | 82 |
| 22 | 10×21 | 121 | 13×22 | 121 | 13×27 | 126 | 13×27 | 132 | 16×33 | 137 | 16×36 | 143 |
| 33 | 13×22 | 154 | 13×27 | 167 | 16×28 | 178 | 16×33 | 186 | 16×36 | 192 | 16×42 | 201 |
| 47 | 13×27 | 198 | 16×33 | 214 | 16×33 | 241 | 16×42 | 253 | 18×42 | 339 | 18×42 | 339 |
| 100 | 16×33 | 345 | 16×36 | 368 | 16×42 | 391 | 22×43 | 402 | 25×43 | 424 | 25×52 | 448 |
| 220 | 18×42 | 586 | 22×43 | 609 | 22×43 | 632 |  |  |  |  |  |  |
| 330 | 22×43 | 632 |  |  |  |  |  |  |  |  |  |  |